## Slide 1
JÖNKÖPING UNIVERSITY
Young's modulus E — how stiff is the material?
Pull the specimen. It stretches. E is how steeply the pull has to rise to keep it stretching.
STRESS = how hard you are pulling ÷ how thick the specimen is. Units MPa.
STRAIN = how much the gauge stretched ÷ how long it was. Just a fraction — no units.
E = how much the STRESS went up, divided by how much it STRETCHED to get there.
RISE = 16.87 - 7.65 = 9.22 MPa
RUN = 0.0040 - 0.0005 = 0.0035
E = 9.22 / 0.0035 = 2634 MPa
2634 MPa = 2.63 GPa. A stiffer material gives a steeper line and a bigger E; a floppier one gives a shallower line.
Steepness of the straight bit = stiffness. Nothing else on the curve is used for E.
V6d · S11 · 100 % infill — the real measurements, not an illustration
1

## Slide 2
JÖNKÖPING UNIVERSITY
The formula the code actually uses
Two points would do — but 101 were measured, so all 101 are used. That is all "least squares" means.
Best-fit slope through all the points:
n·Σ(ε·σ) − Σε · Σσ
E = ─────────────────────────
n·Σ(ε·ε) − (Σε)²
Add up four columns over the 101 points:
n = 101
Σε = 0.237696
Σσ = 1266.1435 MPa
Σ(ε·ε) = 0.000657593
Σ(ε·σ) = 3.238406 MPa
Put the numbers in:
top = 101·3.2384 − 0.2377·1266.14 = 26.1218
bottom = 101·0.0006576 − 0.2377² = 0.0099175
E = 26.1218 / 0.0099175 = 2634 MPa = 2.63 GPa
σ = 2634 × ε + 6.34 R² = 0.9936 the 6.34 MPa offset is the preload the curve starts from, not an error
utm_analysis.analyze() · fit window 0.05 %–0.40 % strain · σ = (F + 470 N anchor) / 80 mm²
2